###### SPTECH Silicon NPN Power Transistor          2N3055

###### DESCRIPTION

·Excellent Safe Operating Area

·DC Current Gain-hFE=20-70@IC = 4A

·Collector-Emitter Saturation Voltage-

: VCE(sat)= 1.1 V(Max)@ IC = 4A

·Complement to Type MJ2955

APPLICATIONS

·Designed for general-purpose switching and amplifier

applications

ABSOLUTE MAXIMUM RATINGS(Ta=25℃)

| SYMBOL | PARAMETER | VALUE | UNIT |
| --- | --- | --- | --- |
| VCBO | Collector-Base Voltage | 100 | V |
| VCER | Collector-Emitter Voltage | 70 | V |
| VCEO | Collector-Emitter Voltage | 60 | V |
| VEBO | Emitter-Base Voltage | 7 | V |
| IC | Collector Current-Continuous | 15 | A |
| IB | Base Current | 7 | A |
| PC | Collector Power Dissipation@TC=25℃ | 115 | W |
| TJ, Tstg | Operating and Storage Junction Temperature Range | -65~+150 | ℃ |

THERMAL CHARACTERISTICS

| SYMBOL | PARAMETER | MAX | UNIT |
| --- | --- | --- | --- |
| Rth j-c | Thermal Resistance,Junction to Case | 1.52 | ℃/W |

###### SPTECH Silicon NPN Power Transistors         2N3055

ELECTRICAL CHARACTERISTICS

TC=25℃ unless otherwise specified

| SYMBOL | PARAMETER | CONDITIONS | MIN | MAX | UNIT |
| --- | --- | --- | --- | --- | --- |
| VCEO(SUS) | Collector-Emitter Sustaining Voltage | IC=30mA ; IB=0 | 60 |  | V |
| VCE(sat)-1 | Collector-Emitter Saturation Voltage | IC= 4A; IB= 0.4A |  | 1.1 | V |
| VCE(sat)-2 | Collector-Emitter Saturation Voltage | IC= 10A; IB= 3.3A |  | 3.0 | V |
| VBE(on) | Base-Emitter On Voltage | IC= 4A ; VCE= 4V |  | 1.5 | V |
| ICEO | Collector Cutoff Current | VCE= 30V; IB=0 |  | 0.7 | mA |
| IEBO | Emitter Cutoff Current | VEB= 7.0V; IC=0 |  | 5.0 | mA |
| hFE-1 | DC Current Gain | IC= 4A ; VCE= 4V | 20 | 70 |  |
| hFE-2 | DC Current Gain | IC= 10A ; VCE= 4V | 5.0 |  |  |
| Is/b | Second Breakdown Collector Current with Base Forward Biased | VCE= 40V,t= 1.0s,Nonrepetitive | 2.87 |  | A |
| fT | Current Gain-Bandwidth Product | IC= 0.5A ; VCE= 10V;f=1.0MHz | 2.5 |  | MHz |